Design of graphene-based TiO2 photocatalysts - A review

Sergio Morales-Torres, Luisa M. Pastrana-Martínez, José L. Figueiredo, Joaquim L. Faria*, Adrián M.T. Silva

Laboratório de Catálise e Materiais (LCM), Laboratório Associado LSRE/LCM, Departamento de Engenharia Química, Faculdade de Engenharia, Universidade do Porto, Rua Dr. Roberto Frias, 4200-465 Porto, Portugal

Abstract:

Because the interest to design high performance photocatalysts using graphene-based materials has increased in the recent years, this review gathers some important aspects of graphene-TiO2 (G-TiO2), graphene oxide-TiO2 (GO-TiO2) and reduced graphene oxide-TiO2 (RGO-TiO2) composites which are of especial relevance as next generation photocatalysts. The methods used for the preparation of these materials, the associated mechanistic fundamentals and the application of graphene-based composites on the photocatalytic degradation of pollutants are reviewed. Some structural, textural and chemical properties of these materials and other photoassisted applications, such as hydrogen production from water splitting and dye-sensitized solar cells, are also briefly included.

Keywords: environment, photocatalyst, graphene, TiO2, composite, synthesis, mechanistic fundamentals, application.

*Corresponding author:

E-mail address: jlfaria@fe.up.pt; Phone: +351-225081645; Fax: +351-225081449.

# Introduction

In the last years, the scientific interest on photocatalysis has increased due to the need of effective photocatalysts and photocatalytic reactor designs for solar applications, the treatment/disinfection of water and air being one of the main research areas (Zhang et al. 2011b; Du et al. 2011b; Pastrana-Martínez et al. 2012a) besides the hydrogen production from water splitting (Silva et al. 2011; Kudo and Miseki 2009; Yu et al. 2011b; Li et al. 2011d; Qi et al. 2011). Other related applications of these materials are also gaining increased importance, such as in solar cells (Roy et al. 2010; Zhu et al. 2011; Yu et al. 2011a), lithium ion batteries (LIBs) (Yang et al. 2011; Li et al. 2011c; Chen et al. 2011), sensors (Fan et al. 2011b; 2011c; 2011d), photocatalytic reduction of CO2 (Liang et al. 2011) and development of substrates with self-cleaning properties (Zhao et al. 2008) and antibacterial or anticancer activity (Akhavan and Ghaderi 2009; Hu et al. 2012).

TiO2 has been broadly used as a usual photocatalyst due to its high stability, low cost, relatively low toxicity and excellent photocatalytic performance in comparison to other semiconductor materials (Leary and Westwood 2011). However, TiO2 presents some particular drawbacks as a limited photoactivity in the visible range of Earth’s solar spectrum. In this context, the typical photocatalysts have been modified in order to enhance their solar photocatalytic activity, by doping, metal particle deposition or even by their combination with other materials to produce highly photoactive composites (Wang et al. 2011b; Liu et al. 2010a).

Among different materials that can be selected to prepare composites with TiO2, carbon materials offers unique advantages such as inert nature and stability, in both acid and basic media, and the possibility to control their textural and chemical properties. Recently, nanostructured carbon materials (carbon nanotubes, fullerenes, graphene nanosheets) have claimed increasing attention in this domain due to their unusual structural and electronic catalytic properties (Sampaio et al. 2011; Yu et al. 2011c; Wang and Zhang 2012). Concretely, graphene has emerged as one of the most promising materials in the next generation of photocatalysts, due to its excellent mobility of charge carriers, a large specific surface area, flexible structure, high transparency and good electrical and thermal conduction. Even so, graphene sheets have a certain tendency to form aggregates in solution by strong van der Waals interactions or hydrogen bonds (in the case of polar solvents). Electrostatic stabilization (Li et al. 2008) and chemical functionalization (Niyogi et al. 2006) are some of the employed methods to avoid these aggregates.

The possibility to obtain graphene from the reduction of graphene oxide (GO), by using simple chemical methods, eases up its application in the synthesis of composite materials at affordable production costs and flexible scalable approaches. By the way, GO can be prepared by strong chemical oxidation of graphite, for instance by using the method developed by Hummers and Offeman (1958), followed by the sonicated-assisted exfoliation of the obtained graphite oxide. For this reason, large scale synthesis of the graphene precursor (GO) is reliable and, as consequence, the entire cycle of the graphene production is estimated to result in low-cost technologies in comparison to those used for preparation of carbon nanotubes (CNT).

General reviews have been published in the field of photocatalysis (Liu et al. 2011c; Chong et al. 2010; Bhatkhande et al. 2002; Han et al. 2009; Thiruvenkatachari et al. 2008) and a specific one dedicated to CNT-TiO2 composites (Woan et al. 2009). Taking into account the growing interest to design graphene-based photocatalysts (Xiang et al. 2012; An and Yu 2011), it is now appropriate in our opinion to present an overview on some important aspects of graphene-based composites, in particular when applied to photocatalysis. The methods of synthesis and the mechanisms proposed so far involving these composites are reviewed. Some structural, textural and chemical insights are also presented. Finally, published works on the photocatalytic degradation of pollutants are collected as well as some other applications where these materials are having strong impact.

# Mechanistic fundamentals of graphene-based photocatalysts

Different terminologies can be found in the literature (G-TiO2, GO-TiO2 and RGO-TiO2) for graphene-based composites prepared with TiO2. The term RGO is explicitly used to refer reduced graphene oxide, this means that the chemical surface of GO composed by different oxygenated surface groups (e.g. epoxy, hydroxyl, ether and carboxylic acids), situated in the basal planes and edges (Stankovich et al. 2006), was reduced by a thermal or chemical treatment. Some authors indicate G-TiO2 even when in certain cases this graphene is obtained from GO (formed during an intermediate step from graphite oxide exfoliation) and, thereby, is more appropriate to define the resulting composite as RGO-TiO2 since it is very unlike to completely reduce GO to pure graphene (oxygenated surface groups usually remain on the graphene sheets after the reduction of GO). In this review, we will use the term G-TiO2 to refer only composites prepared with pure graphene and RGO-TiO2 for those where a reduction of GO is involved.

The first work found in the literature about the preparation of RGO-TiO2 composites by UV-assisted photocatalytic reduction was presented by Williams et al. (2008). They observed how the GO was reduced due to the acceptance of generated electrons from UV-irradiated TiO2 suspensions and proposed a graphene-semiconductor mechanism (Figure 1) that was also verified for ZnO in another study (Williams and Kamat 2009). Briefly, in the presence of ethanol, the photogenerated holes in TiO2 are scavenged to yield ethoxy radicals, leaving the electrons to accumulate within TiO2 particles (eq.1). When GO is present, the accumulated electrons interact with the GO sheets and produce the reduction of certain surface groups - RGO (eq.2).

TiO2+hν→TiO2h++e-C2H5OHTiO2e-+•C2H4OH+H+ 		(1)

TiO2e-+GO→TiO2+RGO 							(2)

Thus, a fraction of electrons is used in the reduction of GO (to obtain RGO) and the other electrons (estimated in ca. 16%) are delocalized throughout π basal planes of GO sheets (Kamat 2010; Lightcap et al. 2010). The reduction of GO can be detected simply by the change of the suspension colour, from light brown (GO) to dark black (RGO), as shown in Figure 1. The colour change is related with the partial restoration of the sp2 hybrid network within the carbon structure (Becerril et al. 2008), which has a beneficial effect because the conductivity loss for GO is recovered when the reduction of the GO sheets takes place.

When these composites are used in the photodegradation of pollutants, different mechanistic pathways have been proposed. Liu et al. (2010b) suggested that the electrons can be transported along the GO sheets and then react with adsorbed O2 to form •OH radicals (Figure 1), which in turn oxidize the pollutant molecules. This interpretation was based on the similar structure of both GO and CNT materials, and considering the work reported by Yu et al. (2005) on CNT and their reactivity with adsorbed O2 to form •OH radicals. Therefore, it is suggested that this effective charge transfer could reduce the charge recombination and increase the photocatalytic activity of TiO2 in GO-TiO2 composites. In a subsequent publication, Liu et al. (2011b) studied the pathway for the photocatalytic degradation of methylene blue (MB) in aqueous solutions using RGO wrapped TiO2 hybrid photocatalysts. They indicated also that RGO acts by capturing photoinduced electrons and MB molecules through an irreversible adsorption process. These MB molecules can be oxidized by the superoxide anion radicals (O2•-) that are produced by the reaction involving dissolved O2 and electrons contained in the RGO surface (eq.3). The holes created in the conduction band of TiO2 could also originate the highly reactive •OH radicals (eq.4, Figure 1).

eCB-+O2→O2•- 									(3)

hVB++H2O→•OH+H+								(4)

Other models have been postulated to explain the role of graphene, GO or RGO in graphene-based TiO2 composites. Chen et al. (2010) observed clearly a p/n heterojuction for RGO-TiO2 composites with p-type semiconductor behaviour, acting GO as a sensitizer and enhancing the visible-light photocatalytic performance. The role of GO as sensitizer was also demonstrated studying the interface between graphene and rutile TiO2 by density functional calculations (Du et al. 2011a). A significant charge was transferred from graphene to TiO2, generating a hole doping in the graphene layer. Thus, under this postulate, electrons can be directly excited from graphene to the conduction band of TiO2 under visible light irradiation.

To design a catalyst combining the properties of a semiconductor material (typically TiO2) and a noble metal (e.g., Au, Pt, or Ag) on the same kind of support is a topic of current research interest, graphene-based materials being used not only in the field of photocatalysis but also in other applications as catalyst supports. The scheme presented in Figure 2a has been proposed as an example of a “photocatalyst mat” with tailored reactive sites for the hydrogen production from water splitting (Kamat 2010; 2011), although it has also a general applicability for other photocatalytic processes (Lightcap et al. 2010). The TiO2 (or other semiconductor) nanoparticle absorbs light and induces the oxidation reaction. Then RGO captures the electrons and shuttles them across the π-π network to the noble metal site, facilitating hydrogen production. The selective anchoring of noble metal particles and TiO2 at separate sites on the surface of RGO, as well the ability of RGO to capture and shuttle the electrons, have been also reported by other authors (Lightcap et al. 2010). Therefore, a graphene-based support acts by capturing photoinduced electrons – due to its excellent electronic properties, these electrons could be shuttled to produce active oxygenated radicals –, or simply by storing them – this being of particular interest for energy applications.

# Methods of synthesis to prepare graphene-based TiO2 composites

According to the literature, TiO2, or other inorganic oxides, with graphene-based nanosheets can be prepared by different methods: simple mixing and/or sonication (Guo et al. 2011; Bell et al. 2011), sol-gel process (Mishra and Ramaprabhu 2011), liquid phase deposition (Jiang et al. 2011b), hydrothermal and solvothermal methods (Fan et al. 2011e; Wang and Zhang 2011; Ding et al. 2011). More information about these methods is presented in the following sections. In addition, a section emphasizing the deposition of metals (e.g. Pt, Ag and Fe) on the composite is also included. In order to offer a useful tool for the reader, Table 1 collects a summary of experimental details regarding the preparation of the composites together with some data on their structural, textural and chemical properties.

## Mixing and sonication

The simplest route for the preparation of GO-TiO2 composites involves mixing and sonication steps, because GO has to be exfoliated when added to an aqueous or organic solution. The method is very common due to its simplicity, but in most cases the interaction between the two phases is weak, since chemical bonding is not expected. In fact, the first reported GO-TiO2 composite was prepared by this method, although a UV-assisted photocatalytic reduction step was also included to obtain RGO-TiO2 (Williams et al. 2008). In the work of Zhang et al. (2011) a heat treatment under inert atmosphere was also applied, after mixing and sonication, which doped carbon atoms into the TiO2 structure and, consequently, improved the visible light photocatalytic activity. In their work, Degussa P25 (now from Evonik) was used to prepare the RGO-TiO2 composites, hereafter referred as RGO-P25. Other visible light active composite photocatalysts were prepared by mixing/sonication but using ZnO (Williams and Kamat 2009) or SnO2 (Paek et al. 2008) nanoparticles, or even WO3 or BiVO4 (Ng et al. 2011), which have a lower conduction band energy than TiO2.

## Sol-gel process

The most widely applied method to obtain an intimate mixing and chemical interaction between GO and TiO2 is the sol-gel technique. The surface of GO nanosheets is generally available to blend with titanium alkoxide precursors, due to the water solubility and hydrogen bonding ability of GO and because the hydroxyl surface groups of GO can establish oxo- or hydroxo-bridges with metal centers. The formation of TiO2 in sol-gel processes involves oxo- or hydroxo-bridges during the hydrolysis of the alkoxides, and finally dispersion by hydroxo-connected GO sheets to form a sol, which evolve into a gel-like biphasic structure with increasing amount of added GO (Manga et al. 2010). Some of the titanium alkoxide species used in the preparation of GO-TiO2 composites were TiCl4 (Akhavan and Ghaderi 2009), TiCl3 (Wang et al. 2009), TiF4 (Lambert et al. 2009), (NH4)2TiF6 (Zhang et al. 2011a), Ti(SO4)2 (Zhang et al. 2011c), Ti(OPri)4 (Peng et al. 2008), Ti(OBu)4 (Wojtoniszak et al. 2012) and titanium peroxo complexes (Václav Štengl et al. 2011; Zou et al. 2011).

However, GO containing aqueous solutions are inadequate for some of these titanium alkoxides that are only dissolved in ethanol sols, the addition of the aqueous GO solution thereby inducing the faster hydrolysis of the ethanol sol and resulting in a rapid precipitation of TiO2. Even so, some precursors such as Ti(OBu)4 could decrease the rate of hydrolysis, because they consist of long side chains, increasing the interaction between GO and the TiO2 materials (Li et al. 2011b).

Some modifications to the sol-gel method have been introduced, including the use of surfactants with the aim to improve the assembly of hydrophobic graphene with hydrophilic TiO2 and to control the nucleation and growth of the resulting nanostructure. Wang et al. (2009) prepared G-TiO2 composites using an anionic sulphate surfactant (sodium dodecyl sulphate, SDS) as template. Chen et al. (2010) used the same methodology to prepare RGO-TiO2 composites that yields different kind of semiconductors depending on the GO content of the starting solution. Manga et al. (2010) proposed the use of an ionic salt, titanium (IV) bis(ammonium lactate) dihydroxide, which has good water solubility and mixes well with GO solutions.

GO-TiO2 composites with more complex structures were also obtained by the sol-gel method when TiO2 nanotubes (Peng et al. 2008) and vertically aligned ZnO nanorod arrays (Akhavan 2010)  were used. Films have been also produced (Manga et al. 2009). Some authors (Jiang et al. 2011b; Zhang et al. 2011a) have used processes based on the sol-gel method but referred as liquid phase deposition for preparation of TiO2 nanoparticles assembled on GO.

## Hydrothermal and solvothermal methods

Both hydrothermal and solvothermal methods involve reactions under controlled temperature and/or pressure, and are usually performed in stainless steel autoclaves. When GO-TiO2 composites are obtained by these methods, GO is partially reduced yielding RGO, or in some cases, graphene sheets if some chemical reagent is added (hydrazine, NaBH4, etc.). In addition, changes in the crystalline phase of TiO2 are generally observed.

Zhang et al. (2010a) reported a hydrothermally prepared RGO-P25 composite, which maintained identical crystalline structure and surface area as P25 and where the original GO was reduced by the effect of the hydrothermal treatment itself. The structure of the resulting composite did not present a good contact, since only some P25 nanoparticles were anchored to the edges of the RGO sheets. In order to overcome this limitation, Liang et al. (2010) prepared a composite by using two-steps, in which TiO2 was first deposited on GO sheets by slow hydrolysis, and then crystallized into anatase nanocrystals by hydrothermal treatment. The slow hydrolysis was induced by the use of an EtOH-H2O (15:1) solution, the addition of H2SO4 leading to the selective growth of TiO2 on GO and suppressing the growth of free TiO2 in solution. In the hydrothermal step, a H2O-dimetilformamide (DMF) solution was used, since DMF facilitates the dispersion of the graphene sheets and reduces their aggregation.

Liu et al. (2011a; 2010b) also obtained composites with homogeneous assembling of TiO2 nanorods on GO sheets through a two-phase approach. The first phase was formed by the dispersion of TiO2 nanorods in toluene and stabilization with oleic acid. The second phase consisted of GO sheets dispersed in deionized water. The self-assembly of both materials occurs at the water/toluene interface. TiO2 nanospindles were also used to obtain graphene-based composites, which were prepared by a hydrothermal process using TiO2 nanotubes as self-sacrificing precursors (Qiu et al. 2010). In this case, the obtained composite was treated in ammonia atmosphere in order to reduce GO to graphene sheets, the TiO2 surface being effectively nitrated.

A variation of the hydrothermal method consists in the addition of glucose, an eco-friendly chemical in comparison with hydrazine, in order to reduce GO to RGO. For instance, a TiO2-RGO composite was prepared using glucose as the reducing agent in a one-step hydrothermal method; however, glucose does not lead to complete reduction under hydrothermal conditions, the reduction mechanism being not yet completely understood (Shen et al. 2011). Fan et al. (2011a) demonstrated that the hydrothermal method is more appropriate than the UV-assisted photocatalytic approach or even than the hydrazine method for GO reduction. In fact, the strongest interaction between both GO and TiO2 materials was obtained using the hydrothermal method.

RGO-TiO2 was also obtained by the solvothermal method employing a GO dispersion and Ti(OBu)4 in isopropanol. For these composites, the carbon basal planes were uniformly covered with TiO2 particles and exhibited a red shift in the UV-Vis absorption spectrum (Zhou et al. 2011) which was already observed for RGO-TiO2 composites obtained by hydrothermal method (Lee et al. 2012). Jiang et al. (2011a) followed a similar solvothermal method and used the same titanium precursor to prepare RGO-TiO2, but in this case HF and methanol were added into the autoclave, leading to composites with exposed {001} facets. A homogeneous growth of TiO2 particles on RGO was obtained by controlling the hydrolysis rate of the Ti(OPri)4 with ethylene glycol and acetic acid (Wang et al. 2011c). A sandwich-like graphene-ZnO composite was also prepared by the solvothermal method in ethylene glycol medium using GO and zinc acetylacetonate, Zn(acac)2, as a single-source precursor of zinc oxide (Wu et al. 2010). The composites presented an increase of the thermal stability and UV-Vis absorption, which was justified by the obtained sandwich-like structure.

## Metal deposition or doping

Metal deposition on G-TiO2 composites is generally used in order to improve the photocatalytic efficiency of the materials. For instance, Pt was deposited on GO-TiO2 composites using H2PtCl6 as platinum precursor and a photochemical reduction method with UV light for 2-3 h under inert atmosphere (Neppolian et al. 2012). Ag/G-TiO2 composite films were prepared by previous immersion of GO-TiO2 composite film in an AgNO3 solution. The reduction of the GO-TiO2 film with Ag+ was achieved with a hydrazine solution (Li et al. 2011a).

TiO2 nanowire arrays doped with Fe were grown on the surface of functionalized graphene sheets by the sol–gel method, using Ti(OPri)4, FeCl3 dissolved in isopropanol and supercritical CO2 as solvent. After calcination at 450 ºC in air, the sample showed a significant reduction in the band gap, from 3.2 eV of the original sample to 2.3 eV of the Fe-doped sample with an optimal Fe content of 0.6%, enhancing the respective  photocatalytic performance (Farhangi et al. 2011).

- Applications

Graphene-based TiO2 composites have been recently used for the photodegradation of pollutants, but they have also been applied in many other fields, including solar cells and hydrogen production, that are related with the preservation of the environment. Table 1 collects some information regarding the details of experiments performed for photocatalytic degradation of pollutants, as well as some of the other related applications.

## Photodegradation of pollutants and microorganisms

The photoinactivation of E. coli bacteria in aqueous solutions under solar light irradiation (Akhavan and Ghaderi 2009) was one of the first applications of GO-TiO2 films, which showed significantly higher efficiencies in comparison to bare anatase TiO2 films (enhancement by a factor of ∼7.5). The better performance was attributed to the suppression of electron–hole recombination, as also proposed by Williams et al. (2008).

In the literature, most of the target pollutants were dyes, such as methylene blue (MB), methyl orange (MO) and rhodamine B (RB), although other compounds (e.g. 2,4-dichlorophenoxyacetic acid (Ng et al. 2010), butane (Václav Štengl et al. 2011), diphenhydramine (Pastrana-Martínez et al. 2012b)) were also used to evaluate the photocatalytic performance of GO-TiO2 composites.

For instance, the degradation of MO under visible light was studied with RGO-TiO2 composites prepared with different GO contents (Chen et al. 2010). The composites with 0.13-0.15 wt.% carbon content were more active than P25, the highest conversion being obtained for a composite prepared with 0.14 wt.% (p-type semiconductor). GO acted as a sensitizer, enhancing the photocatalytic performance towards wavelengths longer than 510 nm. GO-TiO2 composites presented relatively high efficiency after several consecutive cycles for the degradation of MO under UV light, but a decrease of the MO conversion was noticed after each cycle and attributed to the agglomeration of TiO2 grains formed on both sides of the graphene oxide layers (Zhang et al. 2011c). This agglomeration led to a decrease of the contact area between MO molecules and TiO2 particles, also resulting in a reduction of the photodegradation efficiency. The relative stable performance was also confirmed when the composites were exposed to air at room temperature for 4 weeks. However, after 8 weeks, their activity for MO degradation was reduced in ca. 15 %. Similar performance was observed for P25 (Zhang et al. 2011c).

The photocatalytic activity of RGO-P25 composites (1 wt.% GO) was also evaluated in the degradation of MB (Zhang et al. 2010a), a higher conversion of MB being found with these composites than with bare P25, or even with CNT-P25 composites prepared with the same carbon content as GO-P25. This photocatalytic enhancement was ascribed (i) to the two-dimensional planar graphene structure favouring dye absorption, (ii) to the suppression of electron–hole recombination (due to the high electrical conductivity), (iii) to enhanced light absorption in longer wavelengths of the visible region and (iv) to high transparency and band-gap narrowing resulting from the presence of Ti–O–C bonds. In general, the carboxylic acid functional group of GO facilitates binding of oxide particles. The high dye adsorption is due to the formation of both π-π conjugations and the ionic interactions between MB molecules and oxygenated surface groups at the edges or on the surfaces of GO. Moreover, the electron consumption occurs simultaneously, in which GO is partially reduced to RGO under UV assistance and electrons are regenerated, resulting in the partial restoration of the conjugated π-π network (Lightcap et al. 2010; Williams et al. 2008). This phenomenon leads to an efficient charge separation and to the possibility of more π-π interactions between the composite and the organic compounds.

GO-TiO2 composites, prepared with a GO content of 10 wt.% (Liang et al. 2010; Nguyen-Phan et al. 2011), presented a higher activity for the photodegradation of MB under UV irradiation than bare P25 and a GO-P25 composite prepared following the methodology used by Zhang et al. (2010a). This better photocatalytic behaviour was also demonstrated for the degradation of RB, and it was justified by the higher BET surface area of the composites and a stronger contact between TiO2 and GO in comparison to those prepared by the method employed by Zhang et al. (2010a). In fact, the good stability and contact between TiO2 and GO sheets is essential for the effective charge transfer and effective charge separation during the photocatalytic process.

GO-TiO2 nanorod composites presented a large enhancement of MB (Liu et al. 2010b) and acid orange 7 (AO 7) photocatalytic degradation under UV light irradiation and also for E. Coli bacteria under simulated solar light (Liu et al. 2011a). In the same work, the degradation rate of MB in a consecutive second cycle was faster than that observed in the first cycle, due to the reduction of GO under UV light irradiation, while a different adsorption ability of GO sheets was observed for AO 7 and MB, and attributed to the difference in the molecular structure. As expected, the photocatalyst performance also depends on the molecular structure of the pollutant.

The degradation of MB and RB was also studied with composites prepared with TiO2 nanoparticles and pure graphene (only 2-4 layers) as well as boron- and nitrogen-doped graphene (Gopalakrishnan et al. 2011). The mechanism seems to involve the photoexcitation of electrons in the TiO2 nanoparticles followed by their transfer to graphene, as well as interactions of the adsorbed dye molecules with graphene by a π-π and charge transfer interaction (Zhang et al. 2010a). MB, which is a good electron donor, interacts better with hole-doped graphene (boron doped graphene), while RB, which is a poorer electron donor, interacts better with electron-doped graphene (nitrogen doped graphene).

The oxidation of MB was also evaluated under visible light, a conversion 15 times higher than for bare P25 being obtained for G-P25 composites with 1 wt.% graphene content. The electronic structure of pure graphene is strongly associated with its number of layers. In general, a multi-layer graphene becomes a semimetal with a complex band structure in which the conduction and valence bands overlap. This means that graphene can also absorb the visible light, and its excitation electrons are subsequently injected into the conduction band of TiO2, and then transferred to the surface where they react with oxygen to yield superoxide radicals, and directly oxidize MB (Zhang and Pan 2011).

Other alternative to design high performance photocatalysts is the deposition of an active metal on the composite. The photocatalytic degradation of dodecylbenzenesulfonate surfactants (DBS) in aqueous solutions was studied using Pt/GO-TiO2 (Neppolian et al. 2012), which degraded DBS at a higher rate than P25, bare TiO2 or GO-TiO2 photocatalysts. The mineralization of DBS was enhanced by a factor of 3 using Pt/GO-TiO2 with GO content of 0.5 wt.% in comparison with bare P25. It is suggested that Pt acts as a reservoir for photogenerated electrons, promoting an interfacial charge-transfer process. Thus, photoformed electrons can be readily transported through both Pt and GO and the electron–hole recombination could be largely prevented. On the other hand, Ag/G-TiO2 films produced a larger photocurrent under visible light illumination than G-TiO2 films, Ag acting as charge transfer to the graphene sheet (Li et al. 2011a) (Figure 2b). The photocatalytic performance of Fe/G-TiO2 was also evaluated under visible light solar irradiation for the photodegradation of 17β-estradiol. All prepared catalysts with different ratios of Fe were active in the visible region of the solar spectrum, the photocatalytic activity being significantly enhanced with increasing Fe doping levels up to 0.6 wt.%, which decreased the band gap to the visible region (Farhangi et al. 2011), as represented in Figure 2c.

Even if a reasonable amount of work has been already published, there are still some doubts regarding the real enhanced photocatalytic properties of GO-TiO2 composites when compared with other carbon-based TiO2 composites. Zhang et al. (2010c) prepared G-P25 composites with different graphene contents (0.2, 0.5, 1.0, 2.0, 5.0, 10.0 and 30.0 wt.%) and they tested these materials in the photodegradation of benzene, in this case a gas phase application under UV irradiation. The highest photocatalytic activity was obtained for composites prepared with 0.5 wt.% of graphene. Then, the same composites were tested in the photodegradation of MB and MO in liquid phase, under both UV and Vis light irradiation, the highest efficiency being obtained with the composite prepared with 5 wt.% of graphene, regardless of the irradiation source. The authors also prepared CNT-P25 with different CNT contents and tested these materials in the photodegradation of MB. The tendency observed for graphene-based P25 composites was also observed for CNT-P25 composites, although the G-P25 composites exhibited slightly higher activity for degradation of MB than their CNT-P25 equivalents, suggesting than graphene was in essence similar to CNT regarding the obtained photocatalytic performances.

Recently, Zhang et al. (2011d) synthesized again G-TiO2 and CNT-TiO2 composites, but in this case by using a sol-gel method with TiF4. Both types of composites were tested in the photocatalytic selective oxidation of alcohols under visible light irradiation, the G-TiO2 composite with 5 wt.% of graphene showing the best efficiency, which was also much more active than its analogue CNT-TiO2. Therefore, according to the results obtained by Zhang et al. (2010c; 2011d), it can be concluded that the preparation method plays a very important role in affecting or not the photocatalytic performance of graphene-based TiO2 composites.

## Other applications of graphene-based composites

Hydrogen production from water splitting is another application of interest in this area, since the extension of light absorption to the visible light region for development of solar-driven technologies, and the suppression of electron-holes recombination, are also key factors in this process. G-TiO2 composites already showed higher production of hydrogen than P25 (Zhang et al. 2012). The highest photocatalytic activity was obtained with G-TiO2 composites with 5 wt.% of graphene content and treated in a nitrogen atmosphere, whose hydrogen production exceeded more than 2 times that observed for P25, using Na2S and Na2SO3 as sacrificial agents (Zhang et al. 2010b). RGO-P25 composites were also more effective for hydrogen production from methanol aqueous solutions than CNT-P25 or P25 (Fan et al. 2011a). In addition, this RGO-P25 composite (without co-catalyst) yielded a higher hydrogen production rate from pure water than P25, due to the fast transfer of photogenerated electrons on P25 to RGO, suppressing the recombination of charge carriers. Because the photocatalytic activity of anatase TiO2 nanosheets is largely enhanced by the presence of (001) facets (Wen et al. 2011; Xiang et al. 2011b), RGO-TiO2 composites were designed following this approach and showed an excellence photocatalytic behaviour in the hydrogen production, using methanol as sacrificial agent (Xiang et al. 2011a). In this case, the optimum graphene content was ca. 1 wt.%, the yield of hydrogen being 41 times higher than that showed for bare TiO2 and also higher for a RGO-P25 prepared under a similar procedure. Xiang et al. (2011a) ascribed the enhance in the photocatalytic activity to the absolute potential of graphene/graphene·-, which is less negative than the conduction band of TiO2 and more negative than H+/H2 , favouring the electron transfer from TiO2 to graphene and the reduction of H+ and, consequently, the photocatalytic hydrogen production. Lv et al (2012) also collected the good hydrogen-generating capability of RGO-P25 composites and even when compared with well-known Pt co-catalyst.

Technologies based on dye-sensitized solar cells (DSSC) are also promising and present increasing potential for large-scale conversion of sunlight into electrical energy at affordable costs. The photoanodes of DSSCs are typically constructed using thick films of TiO2 nanoparticles, providing anchoring sites for dye molecules. However, electron transport across disordered TiO2 nanoparticles is not yet effective enough, and the recombination of the photogenerated electrons can take place, decreasing the efficiency of DSSCs. Graphene-based TiO2 composites have already been used in the fabrication of DSSC, showing encouraging results (Kim et al. 2009). The incorporation of graphene improves the conductivity by a factor larger than 2, and increases the power conversion by a factor larger than 5, in comparison with TiO2 alone. The better performance of the G-TiO2 composite was also attributed to the better dye loading on the G-TiO2 film than on the TiO2 film (Tang et al. 2010).

- Conclusions

Graphene-based composites can capture photoinduced electrons originated from TiO2 (or other semiconductor) particles. The electrons can be stored in the own π-π network of the composites and can produce the reduction of graphene oxide by themselves. These electrons can also be shuttled to other metal particles deposited on the graphene layer or used to generate active oxygenated radicals. In this way, the carbon material retards the electron–hole recombination on TiO2 and extends the absorption of light to longer wavelengths of the visible region. Additionally, GO can also act as sensitizer, enhancing the photocatalytic efficiency under light-visible irradiation. Different methods of synthesis have been described in the literature, as well as methods to modify the material by metal deposition or doping. The simple mixing of a semiconductor and graphene-based materials usually results in a poor contact between both phases. Sol-gel or hydrothermal methods lead to more intimate contact and enhance the photocatalytic properties of the resulting composite. The photodegradation of pollutants seems to depend on several factors, such as textural (surface area), chemical and morphological properties of the composites, type of interaction between the composite and the pollutant and graphene (pure, oxidized or reduced) content. Graphene-based TiO2 composites presented encouraging results not only in the photocatalytic degradation of pollutants, but also in other applications such as hydrogen production from water splitting and DSSC, LIBs and sensors, but they are still at an early stage of development.

Acknowledgements

Financial support for this work was provided by the European Commission (Clean Water - Grant Agreement nº 227017) and by Fundação para a Ciência e a Tecnologia (FCT) and FEDER under Program COMPETE, project FCOMP-01-0124-FEDER-022706 (Ref. FCT Pest-C/EQB/LA0020/2011) and FCOMP-01-0124-FEDER-008442 (Ref. NANO/NTec-CA/0046/2007). Clean Water is a Collaborative Project co-funded by the Research DG of the European Commission within the joint RTD activities of the Environment and NMP Thematic Priorities. SMT and AMTS acknowledge financial support from SFRH/BPD/74239/2010 and POCI/N010/2006, respectively.

References

Akhavan O, Ghaderi E (2009) Photocatalytic reduction of graphene oxide nanosheets on TiO2 thin film for photoinactivation of bacteria in solar light irradiation. J Phys Chem C 113:20214-20220

An X, Yu JC (2011) Graphene-based photocatalytic composites. RSC Adv 1:1426-1434

Becerril HA, Mao J, Liu Z, Stoltenberg RM, Bao Z, Chen Y (2008) Evaluation of solution-processed reduced graphene oxide films as transparent conductors. ACS Nano 2:463-470

Bell NJ, Ng YH, Du A, Coster H, Smith SC, Amal R (2011) Understanding the enhancement in photoelectrochemical properties of photocatalytically prepared TiO2-reduced graphene oxide composite. J Phys Chem C 115:6004-6009

Bhatkhande DS, Pangarkar VG, Beenackers AACM (2002) Photocatalytic degradation for environmental applications - A review. J Chem Technol Biotechnol 77:102-116

Chen C, Cai W, Long M, Zhou B, Wu Y, Wu D, Feng Y (2010) Synthesis of visible-light responsive graphene oxide/TiO2 composites with p/n heterojunction. ACS Nano 4:6425-6432

Chen JS, Wang Z, Dong XC, Chen P, Lou XW (2011) Graphene-wrapped TiO2 hollow structures with enhanced lithium storage capabilities. Nanoscale 3:2158-2161

Chong MN, Jin B, Chow CWK, Saint C (2010) Recent developments in photocatalytic water treatment technology: A review. Water Res 44:2997-3027

Ding S, Chen JS, Luan D, Boey FYC, Madhavi S, Lou XW (2011) Graphene-supported anatase TiO2 nanosheets for fast lithium storage. Chem Commun 47:5780-5782

Du A, Ng YH, Bell NJ, Zhu Z, Amal R, Smith SC (2011a) Hybrid Graphene/Titania Nanocomposite: Interface Charge Transfer, Hole Doping, and Sensitization for Visible Light Response. J Phys Chem Lett 2:894-899

Du J, Lai X, Yang N, Zhai J, Kisailus D, Su F, Wang D, Jiang L (2011b) Hierarchically ordered macro-mesoporous TiO2-graphene composite films: Improved mass transfer, reduced charge recombination, and their enhanced photocatalytic activities. ACS Nano 5:590-596

Fan W, Lai Q, Zhang Q, Wang Y (2011a) Nanocomposites of TiO2 and reduced graphene oxide as efficient photocatalysts for hydrogen evolution. J Phys Chem C 115:10694-10701

Fan Y, Huang KJ, Niu DJ, Yang CP, Jing QS (2011b) TiO2-graphene nanocomposite for electrochemical sensing of adenine and guanine. Electrochem Acta 56:4685-4690

Fan Y, Liu JH, Lu HT, Zhang Q (2011c) Electrochemical behavior and voltammetric determination of paracetamol on Nafion/TiO2-graphene modified glassy carbon electrode. Colloids Surf B 85:289-292

Fan Y, Liu JH, Lu HT, Zhang Q (2011d) Electrochemistry and voltammetric determination of L-tryptophan and L-tyrosine using a glassy carbon electrode modified with a Nafion/TiO2-graphene composite film. Microchim Acta 173:241-247

Fan Y, Lu HT, Liu JH, Yang CP, Jing QS, Zhang YX, Yang XK, Huang KJ (2011e) Hydrothermal preparation and electrochemical sensing properties of TiO2-graphene nanocomposite. Colloids Surf B 83:78-82

Farhangi N, Chowdhury RR, Medina-Gonzalez Y, Ray MB, Charpentier PA (2011) Visible light active Fe doped TiO2 nanowires grown on graphene using supercritical CO2. Appl Catal B. doi: 10.1016/j.apcatb.2011.08.012

Gopalakrishnan K, Joshi HM, Kumar P, Panchakarla LS, Rao CNR (2011) Selectivity in the photocatalytic properties of the composites of TiO2 nanoparticles with B- and N-doped graphenes. Chem Phys Lett 511:304-308

Guo J, Zhu S, Chen Z, Li Y, Yu Z, Liu Q, Li J, Feng C, Zhang D (2011) Sonochemical synthesis of TiO2 nanoparticles on graphene for use as photocatalyst. Ultrason Sonochem 18:1082-1090

Han F, Kambala VSR, Srinivasan M, Rajarathnam D, Naidu R (2009) Tailored titanium dioxide photocatalysts for the degradation of organic dyes in wastewater treatment: A review. Appl Catal A 359:25-40

Hu Z, Huang Y, Sun S, Guan W, Yao Y, Tang P, Li C (2012) Visible light driven photodynamic anticancer activity of graphene oxide/TiO2 hybrid. Carbon 50:994-1004

Hummers J, Offeman RE (1958) Preparation of graphitic oxide. J Am Chem Soc 80:1339

Jiang B, Tian C, Pan Q, Jiang Z, Wang JQ, Yan W, Fu H (2011a) Enhanced Photocatalytic Activity and Electron Transfer Mechanisms of Graphene/TiO2 with Exposed {001} Facets. J Phys Chem C 115:23718-23725

Jiang G, Lin Z, Chen C, Zhu L, Chang Q, Wang N, Wei W, Tang H (2011b) TiO2 nanoparticles assembled on graphene oxide nanosheets with high photocatalytic activity for removal of pollutants. Carbon 49:2693-2701

Kamat PV (2010) Graphene-based nanoarchitectures. Anchoring semiconductor and metal nanoparticles on a two-dimensional carbon support. J Phys Chem Lett 1:520-527

Kamat PV (2011) Graphene-based nanoassemblies for energy conversion. J Phys Chem Lett 2:242-251

Kim SR, Parvez M, Chhowalla M (2009) UV-reduction of graphene oxide and its application as an interfacial layer to reduce the back-transport reactions in dye-sensitized solar cells. Chem Phys Lett 483:124-127

Kudo A, Miseki Y (2009) Heterogeneous photocatalyst materials for water splitting. Chem Soc Rev 38:253-278

Lambert TN, Chavez CA, Hernandez-Sanchez B, Lu P, Bell NS, Ambrosini A, Friedman T, Boyle TJ, Wheeler DR, Huber DL (2009) Synthesis and characterization of titania-graphene nanocomposites. J Phys Chem C 113:19812-19823

Leary R, Westwood A (2011) Carbonaceous nanomaterials for the enhancement of TiO2 photocatalysis. Carbon 49:741-772

Lee JS, You KH, Park CB (2012) Highly Photoactive, Low Bandgap TiO2 Nanoparticles Wrapped by Graphene. Adv Mater 24:1084-1088

Li D, Müller MB, Gilje S, Kaner RB, Wallace GG (2008) Processable aqueous dispersions of graphene nanosheets. Nat Nanotechnol 3:101-105

Li G, Wang T, Zhu Y, Zhang S, Mao C, Wu J, Jin B, Tian Y (2011a) Preparation and photoelectrochemical performance of Ag/graphene/TiO2 composite film. Appl Surf Sci 257:6568-6572

Li H, Zhang W, Zou L, Pan L, Sun Z (2011b) Synthesis of TiO2-graphene composites via visible-light photocatalytic reduction of graphene oxide. J Mater Res 26:970-973

Li N, Liu G, Zhen C, Li F, Zhang L, Cheng HM (2011c) Battery performance and photocatalytic activity of mesoporous anatase TiO2 nanospheres/graphene composites by template-free self-assembly. Adv Funct Mater 21:1717-1722

Li Q, Guo B, Yu J, Ran J, Zhang B, Yan H, Gong JR (2011d) Highly Efficient Visible-Light-Driven Photocatalytic Hydrogen Production of CdS-Cluster-Decorated Graphene Nanosheets. J Am Chem Soc 133:10878-10884

Liang Y, Wang H, Casalongue HS, Chen Z, Dai H (2010) TiO2 Nanocrystals grown on graphene as advanced photocatalytic hybrid materials. Nano Res 3:701-705

Liang YT, Vijayan BK, Gray KA, Hersam MC (2011) Minimizing Graphene Defects Enhances Titania Nanocomposite-Based Photocatalytic Reduction of CO2 for Improved Solar Fuel Production. Nano Lett 11:2865-2870

Lightcap IV, Kosel TH, Kamat PV (2010) Anchoring semiconductor and metal nanoparticles on a two-dimensional catalyst mat. storing and shuttling electrons with reduced graphene oxide. Nano Lett 10:577-583

Liu G, Wang L, Yang HG, Cheng HM, Lu GQ (2010a) Titania-based photocatalysts - Crystal growth, doping and heterostructuring. J Mater Chem 20:831-843

Liu J, Bai H, Wang Y, Liu Z, Zhang X, Sun DD (2010b) Self-assembling TiO2 nanorods on large graphene oxide sheets at a two-phase interface and their anti-recombination in photocatalytic applications. Adv Funct Mater 20:4175-4181

Liu J, Liu L, Bai H, Wang Y, Sun DD (2011a) Gram-scale production of graphene oxide-TiO2 nanorod composites: Towards high-activity photocatalytic materials. Appl Catal B 106:76-82

Liu J, Wang Z, Liu L, Chen W (2011b) Reduced graphene oxide as capturer of dyes and electrons during photocatalysis: Surface wrapping and capture promoted efficiency. Phys Chem Chem Phys 13:13216-13221

Liu S, Yu J, Jaroniec M (2011c) Anatase TiO2 with Dominant High-Energy {001} Facets: Synthesis, Properties, and Applications. Chem Mater 23:4085-4093

Lv XJ, Fu WF, Chang HX, Zhang H, Cheng JS, Zhang GJ, Song Y, Hu CY, Li JH (2012) Hydrogen evolution from water using semiconductor nanoparticle/graphene composite photocatalysts without noble metals. J Mater Chem 22:1539-1546

Manga KK, Wang S, Jaiswal M, Bao Q, Loh KP (2010) High-gain graphene-titanium oxide photoconductor made from inkjet printable ionic solution. Adv Mater 22:5265-5270

Manga KK, Zhou Y, Yan Y, Loh KP (2009) Multilayer hybrid films consisting of alternating graphene and titania nanosheets with ultrafast electron transfer and photoconversion properties. Adv Funct Mater 19:3638-3643

Mishra AK, Ramaprabhu S (2011) Functionalized graphene-based nanocomposites for supercapacitor application. J Phys Chem C 115:14006-14013

Neppolian B, Bruno A, Bianchi CL, Ashokkumar M (2012) Graphene oxide based Pt-TiO2 photocatalyst: Ultrasound assisted synthesis, characterization and catalytic efficiency. Ultrason Sonochem 19:9-15

Ng YH, Iwase A, Bell NJ, Kudo A, Amal R (2011) Semiconductor/reduced graphene oxide nanocomposites derived from photocatalytic reactions. Catal Today 164:353-357

Ng YH, Lightcap IV, Goodwin K, Matsumura M, Kamat PV (2010) To What Extent Do Graphene Scaffolds Improve the Photovoltaic and Photocatalytic Response of TiO2 Nanostructured Films? J Phys Chem Lett 1:2222-2227

Nguyen-Phan TD, Pham VH, Shin EW, Pham HD, Kim S, Chung JS, Kim EJ, Hur SH (2011) The role of graphene oxide content on the adsorption-enhanced photocatalysis of titanium dioxide/graphene oxide composites. Chem Eng J 170:226-232

Niyogi S, Bekyarova E, Itkis ME, McWilliams JL, Hamon MA, Haddon RC (2006) Solution properties of graphite and graphene. J Am Chem Soc 128:7720-7721

Paek SM, Yoo E, Honma I (2008) Enhanced Cyclic Performance and Lithium Storage Capacity of SnO2/Graphene Nanoporous Electrodes with Three-Dimensionally Delaminated Flexible Structure. Nano Lett 9:72-75

Pastrana-Martínez LM, Faria JL, Doña-Rodríguez JM, Fernández-Rodríguez C, Silva AMT (2012a) Degradation of diphenhydramine pharmaceutical in aqueous solutions by using two highly active TiO2 photocatalysts: Operating parameters and photocatalytic mechanism. Appl Catal B 113-114:221-227

Pastrana-Martínez LM, Morales-Torres S, Likodimos V, Figueiredo J.L., Faria JL, Falaras P, Silva AMT (2012b) Advanced nanostructured photocatalysts based on reduced graphene oxide-TiO2 composites for degradation of diphenhydramine pharmaceutical and methyl orange dye. Appl Catal B under review

Peng W, Wang Z, Yoshizawa N, Hatori H, Hirotsu T (2008) Lamellar carbon nanosheets function as templates for two-dimensional deposition of tubular titanate. Chem Commun:4348-4350

Qi L, Yu J, Jaroniec M (2011) Preparation and enhanced visible-light photocatalytic H2-production activity of CdS-sensitized Pt/TiO2 nanosheets with exposed (001) facets. Phys Chem Chem Phys 13

Qiu Y, Yan K, Yang S, Jin L, Deng H, Li W (2010) Synthesis of size-tunable anatase TiO2 nanospindles and their assembly into Anatase@Titanium oxynitride/titanium nitride-graphene nanocomposites for rechargeable lithium ion batteries with high cycling performance. ACS Nano 4:6515-6526

Roy SC, Varghese OK, Paulose M, Grimes CA (2010) Toward solar fuels: Photocatalytic conversion of carbon dioxide to hydrocarbons. ACS Nano 4:1259-1278

Sampaio MJ, Silva CG, Marques RRN, Silva AMT, Faria JL (2011) Carbon nanotube-TiO2 thin films for photocatalytic applications. Catal Today 161:91-96

Shen J, Yan B, Shi M, Ma H, Li N, Ye M (2011) One step hydrothermal synthesis of TiO2-reduced graphene oxide sheets. J Mater Chem 21:3415-3421

Silva CG, Juárez R, Marino T, Molinari R, García H (2011) Influence of excitation wavelength (UV or visible light) on the photocatalytic activity of titania containing gold nanoparticles for the generation of hydrogen or oxygen from water. J Am Chem Soc 133:595-602

Stankovich S, Dikin DA, Dommett GHB, Kohlhaas KM, Zimney EJ, Stach EA, Piner RD, Nguyen ST, Ruoff RS (2006) Graphene-based composite materials. Nature 442:282-286

Tang YB, Lee CS, Xu J, Liu ZT, Chen ZH, He Z, Cao YL, Yuan G, Song H, Chen L, Luo L, Cheng HM, Zhang WJ, Bello I, Lee ST (2010) Incorporation of graphenes in nanostructured TiO2 films via molecular grafting for dye-sensitized solar cell application. ACS Nano 4:3482-3488

Thiruvenkatachari R, Vigneswaran S, Moon IS (2008) A review on UV/TiO photocatalytic oxidation process. Korean J Chem Eng 25:64-72

Václav Štengl, Daniela Popelková, Petr Vlácil (2011) TiO2-Graphene Nanocomposite as High Performace Photocatalysts. J Phys Chem C 115:25209-25218

Wang D, Choi D, Li J, Yang Z, Nie Z, Kou R, Hu D, Wang C, Saraf LV, Zhang J, Aksay IA, Liu J (2009) Self-assembled TiO2-graphene hybrid nanostructures for enhanced Li-ion insertion. ACS Nano 3:907-914

Wang F, Zhang K (2011) Reduced graphene oxide-TiO2 nanocomposite with high photocatalystic activity for the degradation of rhodamine B. J Mol Catal , A 345:101-107

Wang F, Zhang K (2012) Physicochemical and photocatalytic activities of self-assembling TiO2 nanoparticles on nanocarbons surface. Curr Appl Phys 12:346-352

Wang K, Li HN, Wu J, Ju C, Yan JJ, Liu Q, Qiu B (2011a) TiO2-decorated graphene nanohybrids for fabricating an amperometric acetylcholinesterase biosensor. Analyst 136:3349-3354

Wang P, Han L, Zhu C, Zhai Y, Dong S (2011b) Aqueous-phase synthesis of Ag-TiO2-reduced graphene oxide and Pt-TiO2-reduced graphene oxide hybrid nanostructures and their catalytic properties. Nano Res. doi: 10.1007/s12274-011-0165-2

Wang P, Zhai Y, Wang D, Dong S (2011c) Synthesis of reduced graphene oxide-anatase TiO2 nanocomposite and its improved photo-induced charge transfer properties. Nanoscale 3:1640-1645

Wen CZ, Jiang HB, Qiao SZ, Yang HG, Lu GQ (2011) Synthesis of high-reactive facets dominated anatase TiO2. J Mater Chem 21:7052-7061

Williams G, Kamat PV (2009) Graphene-semiconductor nanocomposites: Excited-state interactions between ZnO nanoparticles and graphene oxide. Langmuir 25:13869-13873

Williams G, Seger B, Kamt PV (2008) TiO2-graphene nanocomposites. UV-assisted photocatalytic reduction of graphene oxide. ACS Nano 2:1487-1491

Woan K, Pyrgiotakis G, Sigmund W (2009) Photocatalytic Carbon-Nanotube-TiO2 Composites. Adv Mater 21:2233-2239

Wojtoniszak M, Zielinska B, Chen X, Kalenczuk RJ, Borowiak-Palen E (2012) Synthesis and photocatalytic performance of TiO2 nanospheres-graphene nanocomposite under visible and UV light irradiation. J Mater Sci 47:3185-3190

Xiang Q, Yu J, Jaroniec M (2011a) Enhanced photocatalytic H2-production activity of graphene-modified titania nanosheets. Nanoscale 3

Xiang Q, Yu J, Jaroniec M (2012) Graphene-based semiconductor photocatalysts. Chem Soc Rev 41:782-796

Xiang Q, Yu J, Wang W, Jaroniec M (2011b) Nitrogen self-doped nanosized TiO2 sheets with exposed {001} facets for enhanced visible-light photocatalytic activity. Chem Commun 47:6906-6908

Yang S, Feng X, Müllen K (2011) Sandwich-like, graphene-based titania nanosheets with high surface area for fast lithium storage. Adv Mater 23:3575-3579

Yu J, Fan J, Cheng B (2011a) Dye-sensitized solar cells based on anatase TiO2 hollow spheres/carbon nanotube composite films. Journal of Power Sources 196:7891-7898

Yu J, Hai Y, Cheng B (2011b) Enhanced Photocatalytic H2-Production Activity of TiO2 by Ni(OH)2 Cluster Modification. J Phys Chem C 115:4953-4958

Yu J, Ma T, Liu G, Cheng B (2011c) Enhanced photocatalytic activity of bimodal mesoporous titania powders by C60 modification. Dalton Trans 40:6635-6644

Yu Y, Yu JC, Chan CY, Che YK, Zhao JC, Ding L, Ge WK, Wong PK (2005) Enhancement of adsorption and photocatalytic activity of TiO2 by using carbon nanotubes for the treatment of azo dye. Appl Catal B 61:1-11

Zhang H, Lv X, Li Y, Wang Y, Li J (2010a) P25-graphene composite as a high performance photocatalyst. ACS Nano 4:380-386

Zhang H, Xu P, Du G, Chen Z, Oh K, Pan D, Jiao Z (2011a) A facile one-step synthesis of TiO2/graphene composites for photodegradation of methyl orange. Nano Res 4:274-283

Zhang J, Xiong Z, Zhao XS (2011b) Graphene-metal-oxide composites for the degradation of dyes under visible light irradiation. J Mater Chem 21:3634-3640

Zhang Q, He YQ, Chen XG, Hu DH, Li LJ, Yin T, Ji LL (2011c) Structure and photocatalytic properties of TiO2-Graphene Oxide intercalated composite. Chin Sci Bull 56:331-339

Zhang X, Sun Y, Cui X, Jiang Z (2012) A green and facile synthesis of TiO2/graphene nanocomposites and their photocatalytic activity for hydrogen evolution. Int J Hydrogen Energy 37:811-815

Zhang XY, Li HP, Cui XL, Lin Y (2010b) Graphene/TiO2 nanocomposites: Synthesis, characterization and application in hydrogen evolution from water photocatalytic splitting. J Mater Chem 20:2801-2806

Zhang Y, Pan C (2011) TiO2/graphene composite from thermal reaction of graphene oxide and its photocatalytic activity in visible light. J Mater Sci 46:2622-2626

Zhang Y, Tang ZR, Fu X, Xu YJ (2010c) TiO2-graphene nanocomposites for gas-phase photocatalytic degradation of volatile aromatic pollutant: Is TiO2-graphene truly different from other TiO2-carbon composite materials? ACS Nano 4:7303-7314

Zhang Y, Tang ZR, Fu X, Xu YJ (2011d) Engineering the unique 2D mat of graphene to achieve graphene-TiO  nanocomposite for photocatalytic selective transformation: What advantage does graphene have over its forebear carbon nanotube? ACS Nano 5:7426-7435

Zhao X, Zhao Q, Yu J, Liu B (2008) Development of multifunctional photoactive self-cleaning glasses. J Non-Cryst Solids 354:1424-1430

Zhou K, Zhu Y, Yang X, Jiang X, Li C (2011) Preparation of graphene-TiO2 composites with enhanced photocatalytic activity. New J Chem 35:353-359

Zhu G, Xu T, Lv T, Pan L, Zhao Q, Sun Z (2011) Graphene-incorporated nanocrystalline TiO2 films for CdS quantum dot-sensitized solar cells. J Electroanal Chem 650:248-251

Zou F, Yu Y, Cao N, Wu L, Zhi J (2011) A novel approach for synthesis of TiO2-graphene nanocomposites and their photoelectrical properties. Scr Mater 64:621-624

TABLE

Table 1. Experimental procedures and applications of graphene-based TiO2 composites in the literature.

| Method of synthesis | Precursors | Preparation details | Relevant characteristics (morphology, *SBET, phase crystalline) | Application tested | Ref. |
| --- | --- | --- | --- | --- | --- |
| Mixing | Ti(OPri)4 GO solid | GO was added to a TiO2 suspension in ethanol and then sonicated for 30 min. RGO-TiO2 was obtained by UV-assisted photocatalytic reduction, under continuous stirring and N2 flow | Height of ~ 2 nm for RGO sheet and a particle diameter for TiO2 of 2-7 nm | - | (Williams et al. 2008) |
| Mixing | Ti(OPri)4 GO dispersion | TiO2 nanorods were synthetized using oleic acid as surfactant by a hydrothermal method (180 ºC, 6 h). Then, they were dispersed in toluene and mixed with a GO aqueous dispersion for 24 h. Finally, the composite was purified and washed with acetone, THF and freeze-dried at -50 ºC for 48 h | Anatase TiO2 nanorods of 2-4 nm diameter and 20-30 nm length | Photodegradation of MB (0.2 gTiO2 L-1, 10 ppm MB) under UV light irradiation (254 nm, 11 W) | (Liu et al. 2010b) |
| Mixing | P25 GO dispersion | P25 was added to the GO dispersion. The mixture was sonicated for 1 h and treated in Ar flow at 300 ºC for 2 h | TiO2 particles with anatase and rutile phases. SBET = 79 m2 g-1 | Photodegradation of MB (1 gcat L-1, 12 ppm MB) under Vis light irradiation (250 W, high pressure Hg lamp and cutoff filter, λ>400 nm | (Zhang and Pan 2011) |
| Sol-gel | TiCl4 GO dispersion | TiO2 films were prepared and treated at 450 ºC for 1 h. A GO dispersion was spreading on the TiO2 film and then dried at 60 ºC for 24 h and post-annealed in air at 400 ºC for 30 min and UV-assisted photocatalytic reduction | TiO2 films with anatase phase | Photodegradation of E. coli bacteria (~108 CFU mL-1) in a saline solution under solar light irradiation | (Akhavan and Ghaderi 2009) |
| Sol-gel | (NH4)2TiF6 GO dispersion | (NH4)2TiF6 and H3BO3 were added to a GO dispersion and the mixture was heated at 60 ºC for 2 h. The solid was thermally treated in air flow at 200 ºC for 1 h | TiO2 particles with anatase phase. SBET = 80 m2 g-1 | Photodegradation of MO (0.5 gcat L-1, 10 ppm MO) under UV light irradiation (20 W, UV lamp) | (Jiang et al. 2011b) |
| Sol-gel | TiCl3 Graphene sheets | An anionic surfactant (SDS) was added during sol-gel method. Composites were treated in air flow at 400 ºC for 2 h. The formation of anatase TiO2 particles is favoured by adding sodium sulfate together with SDS | Anatase and rutile TiO2-GO composites | Li-ion batteries | (Wang et al. 2009) |
| Sol-gel | TiCl3 GO dispersion | Methodology similar to (Wang et al. 2009) but GO is used instead of graphene. The composites were purified by centrifugation-washing-redispersion cycles | Anatase TiO2 particles with a crystal size of 6-8 nm. Band gap < 2.43 eV. | Photodegradation of MO (1 gcat L-1, 12 ppm MO) under Vis light irradiation (1000 W Xenon lamp) and cutoff filter, λ>400 nm | (Chen et al. 2010) |
| Sol-gel | TiF4 GO dispersion | TiF4 was added to an GO aqueous dispersion and the mixture was heated at 60 ºC for 24 h to prepare GO-TiO2 composites. RGO-TiO2 composites were also prepared by heating GO-TiO2 (1000 ºC) and chemical reduction using hydrazine hydrate at 100 ºC | Anatase TiO2 nanocrystals and SBET = 121 m2 g-1. RGO-TiO2 chemically reduced presented higher SBET and a anatase-rutile phase for TiO2 particles | - | (Lambert et al. 2009) |
| Sol-gel | Ti(SO4)2 GO dispersion | GO dispersion was added to an aqueous solution formed by adding Ti(SO4)2 and H2SO4. The mixture was heated at 80 ºC for 2 h | TiO2 crystallites of mixed antase and rutile phases. Average crystal size of TiO2 was about 9 nm | Photodegradation of MO (1 gcat L-1, 20 ppm MO) under UV light irradiation (250 W, high pressure lamp) | (Zhang et al. 2011c) |
| Sol-gel | Ti(BuO)4 Graphene dispersion | Ti(BuO)4 was added to a GO ethanolic dispersion. After curing for 2 days acetic acid was added and the cure was prolonged for other 2 days and then the mixture was dried at 80 ºC for 10 h. Composites were treated in air flow at 450 ºC for 2 h | Anatase TiO2 nanoparticles with a size ca. 10-15 nm. SBET = 37 m2 g-1 | Hydrogen evolution from water splitting under UV-Vis light irradiation (500 W Xe lamp) and using 0.1 gcat. | (Zhang et al. 2010b) |
| Hydrothermal | P25 GO dispersion | GO dispersion (1 wt.%) in water-ethanol (2:1) was sonicated for 1 h. P25 was added to the GO dispersion and then added in an autoclave at 120 ºC for 3 h | Anatase-rutile phases (80%-20%) for TiO2 particles. SBET = 50 m2 g-1 | Photodegradation of MB (0.01 gcat L-1, 2.7·10-5 M MB, under UV (100 W high pressure Hg lamp) or Vis light irradiation (500 W Xe lamp and cutoff filter, λ>400nm) | (Zhang et al. 2010a) |
| Hydrothermal | Ti(BuO)4 GO | Ti(BuO)4 , GO and H2SO4 were added to a EtOH-H2O solution (15:1 v/v), heated at 80 ºC and dried. The composite was added to a H2O-DMF solution and added in an autoclave at 200ºC | Anatase TiO2 nanocrystals. SBET = 190 m2 g-1 | Photodegradation of RB and MB under UV light irradiation | (Liang et al. 2010) |
| Hydrothermal | Ti(BuO)4 GO dispersion | Ti(BuO)4 and NH4Cl were added to an ethanol-H2O solution. Glucose and NH4OH were added to a GO aqueous dispersion. Both solutions were mixed into an autoclave and heated at 160 ºC for 4 h | Anatase TiO2 nanoparticles with 9 nm size. GO was partially reduced, yielding RGO | - | (Shen et al. 2011) |
| Hydrothermal | P25 GO solid | TiO2 nanotubes were prepared by adding P25 to a NaOH (10 M) aqueous solution, treated in an autoclave at 150 ºC for 12h and washed with 0.1 M HCl aqueous solution. TiO2 spindles were produced by adding TiO2 nanotubes to a water-EtOH-ethylene glycol solution, addition of dimethylamine and heating in an autoclave at 180 ºC for 12h. The GO-TiO2 spindles were obtained by adding GO during the preparation step of TiO2 spindles | Anatase TiO2 spindles with a diameters as low as 5 nm and lengths of ca. 15 nm | Li-ion batteries | (Qiu et al. 2010) |
| Hydrothermal | TiCl4 GO dispers. | TiCl4 and GO aqueous solution were added into an autoclave and heated at 180 ºC for 6 h. The composites were washed with water at 50 ºC for 2 days | Anatase or rutile crystallites were obtained for composites with 0.8-2.0 wt.% or 5.0-10.0 wt.% GO content, respectively | Hydrogen evolution from water splitting under UV-Vis light illumination (500 W Xe lamp). Na2S and Na2SO3 solutions were used together with 25 gcat L-1 | (Zhang et al. 2012) |
| Solvothemal | Ti(BuO)4 GO solid | GO was sonicated in an isopropanol solution. Ti(BuO)4 was added to the GO dispersion and then water dropwise. The mixture was kept in an autoclave and heated at 180 ºC for 8 h | Anatase TiO2 particles with a narrow size distribution | Photodegradation of MB (1 gcat L-1, 10-5 M MB) under sunlight irradiation ( 150 W high pressure Xe lamp) | (Zhou et al. 2011) |
| Solvothermal | Zn(acac)2 GO solid | Both reagents were dispersed in ethylene glycol and sonicated for 30 min. The suspension was reduced with hydrazine and heated in an autoclave at 180 ºC for 16 h | A sandwich-like structure was obtained for ZnO nanoparticles with a diameter of ca. 5 nm | - | (Wu et al. 2010) |

*The referred SBET value is the highest among the graphene-based TiO2 composite presented in the respective work.

FIGURE CAPTIONS

Figure 1. TiO2 nanoparticles attached onto a graphene-based sheet and generation of •OH radicals from adsorbed oxygen and H2O. Illustration of the colour change between GO and RGO by UV assisted reduction.

Figure 2. Electron shuttling on a graphene-based sheet with different active metals supported (Pt, Ag) or doped (Fe) in different catalytic sites: a) Pt (Pt/GO-TiO2) for hydrogen evolution from water splitting, b) Ag for transfer charge in Ag/G-TiO2 films and c) Fe (Fe doped G-TiO2) for enhancement of the visible photocatalytic reactivity.

Figure 1.

Figure 2.